## Slide 1: Film Optical Properties
Formulation | NP Film Loading (wt%) | Formulation Viscosity (cP) | Film Thickness (um) | L* | a* | b* | %Haze | YTrans | Film RI (589 nm)
PixNIL SFT1 | 70 | 630 | 7.39 | 97.39 | -0.22 | 1.50 | 0.03 | 93.40 | 1.85
Chart: Film %Transmission
Chart: Film Refractive Index
| 350 | 360 | 370 | 380 | 390 | 400 | 410 | 420 | 430 | 440 | 450 | 460 | 470 | 480 | 490 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 610 | 620 | 630 | 640 | 650 | 660 | 670 | 680 | 690 | 700 | 710 | 720 | 730 | 740 | 750 | 760 | 770 | 780 | 790 | 800 | 810 | 820 | 830 | 840 | 850
 | 1.995 | 1.9834 | 1.9727 | 1.9629 | 1.9538 | 1.9454 | 1.9376 | 1.9304 | 1.9236 | 1.9173 | 1.9115 | 1.906 | 1.9008 | 1.896 | 1.8914 | 1.8872 | 1.8831 | 1.8793 | 1.8758 | 1.8724 | 1.8692 | 1.8662 | 1.8633 | 1.8606 | 1.858 | 1.8555 | 1.8532 | 1.8509 | 1.8488 | 1.8468 | 1.8449 | 1.843 | 1.8413 | 1.8396 | 1.838 | 1.8364 | 1.8349 | 1.8335 | 1.8322 | 1.8309 | 1.8296 | 1.8284 | 1.8273 | 1.8261 | 1.8251 | 1.824 | 1.823 | 1.8221 | 1.8212 | 1.8203 | 1.8194

## Slide 2: Film Conditions
Films were made on 2.5” square glass substrates
Spin-coating
  3,000 RPM/45 sec for 12 um films
  6,000 RPM/45 sec for 7 um films
UV Curing
  365 or 385 UV LED
  2 J/cm2
  N2 atmosphere
Note: These are recommended conditions based on Pixelligent equipment. Film processing can be adapted to suit other application methods and cure conditions.